## Slide 1
Printing
Curing
Excavation and Preprocess
Partical Bed
(Each particle layer: 3.0 mm)
Building Platform
(lowered by 3.0 mm to print a new layer)
Nozzle
(conical and round, inner diameter 2.0 mm)
Moves with the speed of 2000 mm/min on
Output cement paste from reservoir
Hold by
24 hours on the partical bed
Lifted out of the particle bed
Climate Chamber
(20/65; 28 days)
Send to